## Slide 1: The Role of Slag Cement in Creating Sulfate Resistance
www.SlagCement.org

## Slide 2: Overview
What is Sulfate Attack?
Identifying Concrete and Environmental Risk Factors
Managing The Risk of Sulfate Attack In Concrete
Properties of Slag Cement - Benefits in Mitigating Sulfate Attack
Example of a Concrete Field Exposure Site

## Slide 3: What Is Sulfate Attack?
The term used to describe a series of chemical or physical reactions between sulfate ions and the components of hardened concrete, principally the cement paste, caused by exposure of concrete to sulfates and moisture.
If all of these conditions are met in substantial quantity, there is a risk for Sulfate Attack
Sulfate Ions
Water
C3A & CaOH
Chemical Sulfate Attack
Is this oversimplification?
Accessibility To Paste
Sulfate Ions
Water
Absorption Into Concrete
Physical Sulfate Attack
Wetting / Drying Action
In Other Words
Skalny, et al. 2002

## Slide 4: Types of Sulfate Attack
Chemical
Physical
Sulfate reacts with hydration product of C3A and CaOH forming ettringite
Also referred to as
salt crystallization
Ettringite expands to causing distress in hardened concrete
Tends to occur in arid zones
e.g. Western U.S. / Canada
Wicking of sodium sulfate and water into concrete followed by wetting and drying action
Also referred to as
classical sulfate attack

## Slide 5: Sources of Sulfate
Internal
External
Source of Sulfate supplied from external source
Source of Sulfate contained in mixed concrete
Excess sulfate in cement / SCMs
Sulfate rich aggregate
Contamination
Sea, brackish & ground water
Wastewater
High sulfate soils
Examples:
Classic ettringite attack
DEF (special case)
Examples:
Classic ettringite attack
Salt crystallization
Thaumasite

## Slide 6: What Does Sulfate Attack Look Like?
Thaumasite
Chemical
Physical
DEF / ASR

## Slide 7: Identifying Risk for Sulfate Attack
Understand the source and quantity of sulfate in the environment

## Slide 8: Sulfate In Soils and Water
From ACI 318 – Building Code
All Seawater is designated category S1?
Exposure Category | Sulfates In Soil (% by Mass) | Sulfates In Water (ppm)
S0 | < 0.10 | < 150
S1 | 0.10 – 0.20 | 150 – 1500 & seawater
S2 | 0.20 – 2.00 | < 1500 – 10,000
S3 | > 2.00 | > 10,000

## Slide 9: Sulfate Exposure Class of Sea Water
Why is all seawater designated exposure class S1?
Especially when seawater sulfate levels vary substantially by location
Corrosion of steel is a bigger problem & C3A slow ingress of chlorides through binding
Higher exposure classes steer specifier toward Type V and HS cement (lower C3A)
Question
Answer

## Slide 10: Composition of Portland Cement
  Type I
  Type II
  Type II(MH)
  Type III
  Type IV
  Type V
  General use
  Moderate sulfate resistance
  Moderate sulfate & Moderate Heat
  High early strength
  Low heat of hydration
  High sulfate resistance
Clinker (91.4%)
Gypsum (5.2%)
Limestone (2.7%)
IPA (>1%)
Portland Cement
Standard portland cement types
Each type intended to address a specific performance or durability characteristic
Source: Portland Cement Association’s 2021 Portland Cement EPD

## Slide 11: Blended Hydraulic Cement
Clinker (82.7%)
Gypsum (5.7%)
Limestone (10.8%)
IPA (>1%)
Blended cement types
  Type IS
  Type IP
  Type IL
  Type IT
  Portland blast-furnace slag cement
  Portland-pozzolan cement
  Portland-limestone cement
  Ternary blended cement
Each type indicates the cement composition
Source: Portland Cement Association’s 2021 Portland-Limestone Cement EPD
Designations for special properties
  (MS)
  (HS)
  (HE)
  (MH)
  (LH)
  (A)
  Moderate sulfate resistance
  High sulfate resistance
  High early strength
  Moderate heat of hydration
  Low heat of hydration
  Air entraining is required
Type IL Cement
Notes: Portland-limestone blended cement composition example

## Slide 12: Blended Hydraulic Cement – Naming Practice
  Type IT(L10)(S40)(HS)
In ternary blends component designations are listed alphabetically
Portland Cement
  Type IS(60)(LH)
  Type IL(12)(MS)
Blended With Limestone
10% Limestone Target
Moderate Sulfate Resistance
Portland Cement
Portland Cement
Portland Cement
Blended With Limestone
Blended With Slag
12% Limestone Target
60% Slag Target
Blended With Limestone & Slag
Low Heat
10% Limestone Target
40% Slag Target
High Sulfate Resistance
  Type IL(10)

## Slide 13: Identifying Risk for Sulfate Attack
Understand vulnerabilities of concrete mixture to sulfate attack
Utilize established guidelines and or laboratory evaluation of mix design and constituents

## Slide 14: Evaluating Cement and SCM’s – ASTM C1012
Test summary
Used to evaluate sulfate exposures (expansion) of combinations of Portland & blended cement, pozzolan, and slag cement
Mortar bar test with fixed W/C ratios
Air entrained concrete: 0.460
Non air entrained concrete: 0.485
Mortar bars stored in Na2SO4 solution and measured for length change over time (6 to 18 months)

## Slide 15: Interpreting C1012 Results
Exp. Class | Max w/cm | Min f’c psi | Cementing Materials | Performance Requirements in ASTM C1012 (max %) |  | 
 |  |  |  | 6 m | 12 m | 18 m
S0 | No Requirements |  |  |  |  | 
S1 | 0.55 | 3500 | Performance test only  | 0.05 | 0.10 | -
 | 0.50 | 4000 | Type II or Type MS blended cements | 0.10 | - | -
 | 0.45 | 4500 | No restriction | - | - | -
S2 | 0.50 | 4000 | Performance test only  | - | 0.05 | 0.10
 | 0.45 | 4500 | Type V or HS-designated cements | 0.05 | 0.10 | -
 | 0.40 | 5000 | Type II or Type MS | 0.10 | - | -
S3 | 0.45 | 4500 | Performance test only  | - | 0.05 | 0.10
 | 0.40 | 5000 | Type V or HS designated cements | 0.05 | 0.10 | -

## Slide 16: Managing The Risk of Sulfate Attack
Reduce cement C3A content
Reduction of paste permeability
Preventative Measures
Use SCMs at suitable replacements
Utilize Type II & V cement or Type MS & HS blended cement to reduce C3A available to attack
Lower W/Cm ratio, SCMs, adequate curing can greatly reduces ability of sulfates to penetrate into concrete
SCMs like slag cement, Class F ash, silica fume contribute to reduction of overall C3A, permeability and utilize excess CaOH

## Slide 17: All SCMS Are Beneficial To Mitigate Sulfate Attack, Right?
Not So Fast!

## Slide 18: W/C Ratio and Sulfate Attack Resistance
W/Cm Ratio plays a big role in reduction of permeability
Stark PCA, Sacramento Site 1990
Samples after 12 years

## Slide 19: Delayed Ettringite Formation
A special case of internal sulfate attack
Formation of ettringite at late ages due to elevated curing temperatures in excess of 158 f (70 c) at early ages
Formation of late age ettringite can cause expansion and cracking and ultimately deterioration of concrete
Occasionally associated with alkali silica reaction ASR
Ramlochan 2003
If sufficient SCMs used, early age temperatures up to 185 f (85 c) are acceptable – ACI 201.2R-16

## Slide 20: What Is Slag Cement?
A fine white powder that can be used as a SCM to enhance the properties of concrete
In the presence of moisture exhibits hydraulic properties similar to portland cement
Where does it come from?
Non-metallic molten material (slag) is diverted from the waste stream of iron ore blast furnace
Rapidly quenched to produce a glassy granulated product
Slag
Slag
Cement

## Slide 21: What Is Slag Cement?
Slag Granules
Granules are ground to a suitable fineness
Typically finer than portland cement
Can be used in concrete mixtures to enhance durability and sustainability
Microscopic View Of Slag Cement
Slag Cement Grinding Facility

## Slide 22: Slag Cement Reaction
Portland Cement
Concrete System
Portland-Slag Cement
Concrete System
Portland Cement
Slag Cement
Voids
and
CaOH
CSH
Aggregate
Aggregate
Notes: Schematically, the picture on the left shows what happens when ordinary portland cement (gray) hydrates. Calcium-silicate hydrate is formed (yellow), but there are significant areas where this “glue” is not present (voids).
The picture on the right shows that with slag cement (white), much more of the paste is filled with the Calcium Silicate Hydrate. The volume of voids is significantly reduced.
The increased formation of calcium silicate hydrate gives concrete made with slag cement more strength and reduces its permeability.
Greater bond is also formed with the aggregate particles, thus enhancing strength, particularly tensile/flexural strength. (Check Seattle presentation data on flexural strength info)

## Slide 23: Reduced Permeability
What is permeability?
  Measure of how easy it is for water, air and other substances such as chloride ions to enter concrete
  Commonly measured by ASTM C1202 Test Method for Rapid Chloride Permeability
How does slag cement affect permeability?
  Slag cement reacts with calcium hydroxide CaOH to create calcium silicate hydrate CSH reducing permeability
  Low permeability can be achieved in binary and ternary systems with 25 to 65% replacement rates
Why is it important?
  Low permeability concrete can reduce corrosion potential of embedded reinforcing steel

## Slide 24: Effect of Slag Cement on Sulfate Resistance
Chart: Age, days
| 0 | 7 | 14 | 21 | 28 | 56 | 91 | 105 | 120 | 180 | 270 | 365
OPC | 0 | 0.009 | 0.011 | 0.0148 | 0.0198 | 0.0284 | 0.0384 | 0.0414 | 0.0434 | 0.0612 | 0.09225
25% Slag Cement | 0 | 0.0083333 | 0.010833 | 0.014833 | 0.016833 | 0.026167 | 0.0295 | 0.03 | 0.03 | 0.034333 | 0.0342 | 0.0396
50% Slag Cement | 0 | 0.01 | 0.010167 | 0.011833 | 0.014333 | 0.020833 | 0.026667 | 0.031667 | 0.031833 | 0.031833 | 0.032667 | 0.032667
180-day Limit | 0.05 | 0.05
1-year Limit | 0.1 | 0.1

## Slide 25: Slag Cement and Delayed Ettringite Formation
Ramlochan 2003
Deleterious expansion > 0.10%
As little as 25% slag cement completely eliminated DEF
Samples cured at 203 f (95 c) initially then stored in water for 2.5 years
Type III with 0-50% slag cement replacement cured at 203 f (95 c)

## Slide 26: ACI 233R-17 Guide to the Use of Slag Cement in Concrete and Mortar
Type I Cement (C3A = 11.8%) and
various slag cement replacement
Type II Cement and
various slag cement replacement

## Slide 27
ACI 233R-17 Guide to the Use of Slag Cement in Concrete and Mortar
Require high sulfate resistance but limited on low C3A cement?

## Slide 28: Toronto: Concrete Field Sulfate Exposure site
Slag Cement mitigating Sulfate Attack in the Field
2010: trench 8 ft deep prepared for exposure site
Variable annual temperature of 37-61 degrees f.
Test Specimens were concrete prisms 3x 3x 11 in.
Na2SO4 (sodium sulfate) concentration 15,000 ppm
Numerous mixture combinations tested
Type IL(10.5) blended cement with 40 & 50% slag cement
  Type IL C3A = 11%
Type V (high sulfate resistance) without SCM
0.40 Water to Cementitious Ratio

## Slide 29
Slag Cement mitigating Sulfate Attack in the Field
33 months later…
C595 Type IL(10.5) + 40% Slag
C150 Type V (2)
C595 Type IL(10.5) + 50% Slag
C150 Type V (2)
Minor damage
Minor damage
Minor damage
Excellent Condition
Type IL with 40% slag cement comparable to Type V cement
Type IL with 50% slag cement showing better performance to Type V cement

## Slide 30
Slag Cement mitigating Sulfate Attack
How about 38 years of sulfate exposure?
Alapour & Hooton, 2017
Laboratory example of long-term exposure

## Slide 31
Questions?